RBSP EFW

Opamp AD822 TID

Test Report

RBSP_EFW_TR_011

David Curtis, U.C. Berkeley RBSP EFW Systems Engineer

# Document Revision Record

| Rev. | Date | Description of Change |
| --- | --- | --- |

Distribution List

| Name | Email |
| --- | --- |
| David Curtis, Systems Keith Goetz, PM John Bonnell, Inst CoI Jane Hoberman, BEB EE Ron Jackson, QA | dwc@ssl.berkeley.edu goetz@umn.edu jbonnell@ssl.berkeley.edu jch@ssl.berkeley.edu ronj@ssl.berkeley.edu |

TBDs

| Identifier | Description |
| --- | --- |

Reference Documents

| Ref | Doc Number | Title |
| --- | --- | --- |

# Overview

A Total Ionizing Dose radiation test was performed for the RBSP EFW project on five AD822AN (Lot Date Code 0847) opamps at National Semiconductor Gamma cell 220 radiation facilities in Santa Clara, CA, on September 10, 2009.   Opamps were tested at 13 and 20 krads (Si), and after 24 hour room temperature anneal, and finally after a 168 hour at 100C biased anneal.   Some parametric changes were seen during test (particularly at 20krads), most of which were reversed by anneal.  All devices were in spec post-anneal except some small exceeedances of the bias current spec.

# Test Procedure

The devices were characterized prior to radiation and immediately after each dose (and after the anneal periods) using the opamp characterization setup described in section 2.1.  The units were biased during dosing at +/-10V (20mA limit) using the circuit shown in Figure 1.  The 5 parts were radiated simultaneously, and the total supply current was monitored during the test – aome increase in current was seen corresponding to the measured supply current increase in the post-test data.  Parts were dosed at a rate of 156 rads/sec.

Figure 1 – Biasing circuit

## Opamp Characterization

At each step in testing the opamps were fully characterized using an LTS2020 test station with an LTS2100 Opamp family board and an LTS0614 low leakage socket adapter (calibrated Test Tech, 5/21/2008).  This test station makes the following measurements (with the listed accuracies) and verifies the results are within the data sheet specifications.  The values of the parameters are also recorded to look for any significant charges.

Figure 7.  LTS2020  OPAMP  Tester

Test 1.  V+ supply operating current

±0.2% + 10μA

Test 2.  V- supply operating current

±0.2% + 10μA

Test 3,4.  Offset voltage

±0.25% + 5μV

Test 5,6,7,8.  Bias Current

±5% + 25fA

Test 9,10.  Offset Current

±5% + 25fA

Test 11,12.  Large Signal Voltage Gain

±1.5% + 1V/mV

Test 13,14.  Common Mode Rejection Ratio

±0.25% + 0.1dB

Test 15,16.  Power Supply Rejection Ratio

±0.25% + 1μV/V

Test 9,10,11,12.  Output Voltage Swing, 10kohm load

±0.4% + 1mV

Test 13,14,15,16.  Slew Rate

±10%

Test 17,18.  Gain Bandwidth Product.

±10% + 10kHz

Appendix A includes part of the AD822 data sheet showing the operating limits for comparison.

A control part (unit C1) was measured prior to measurements of the TID test devices to verify that any change is not a result of a change in the LTS2020.  Each unit was measured twice.  All testing was done at room temperature.

The tester was initially set to measure within the data sheet limits.  When a parameter exceeded those limits, the limits were expanded in order to measure the actual value without saturation.

# Test Results

The units were all in spec prior to radiation dosing.  Some parametric changes were seen, particularly on IB.  After 13krads IB, IS, and VOS were out of data sheet spec but within acceptable ranges for the RBSP EFW application.  After 20krads the parts still operated but were even further out of spec, now out of spec for PSRR and Vout.  Vout was sufficiently bad to not meet the RBSP EFW requirements.  After 24 hours room temperature anneal the parts were still out of spec but better.  Vout was still marginal for RBSP EFW needs.  After the 168h 100C anneal the parts were all returned to within spec except for IB, which was slightly out of spec for some parts but well within acceptable limits for RBSP EFW use.

Detailed measurement results are presented in Appendix B.

Appendix A – AD822 Data Sheet

# Appendix B -  AD822 Test Results